## Slide 1: Strengthening Origami Structures with Layer Jamming
Presented by: Sana Pournaghshband
Partners: Jordanna Ebanks, Charles Xiao
December 19, 2017

## Slide 2: Layer Jamming Overview
Concept originated at MIT for surgical robots
Project Inspired by jamSheets
  A project by the Tangible Media Group at MIT
Layer jamming happens when many sheets are compressed together
Notes: n is the number of sheets. There are n-1 contacts between n sheets. Mu is the coef of friction. is the pressure gradient between the inside and outside of the vacuum gradient. S is the surface area.
n is the number of sheets. There are n-1 contacts between n sheets. Mu is the coef of friction. ∆𝑃 is the pressure gradient between the inside and outside of the vacuum gradient. S is the surface area.

## Slide 3: Examples of Layer Jamming
Notes: From Top left and then counter clock wise: Chair from jam sheets; linear brake resesearch at Stanford; surgical robot that started it all

## Slide 4: Project Overview
Bending test on different perforation ratios
Miura tensile Test
Pop through test on Hypar
  Only qualitative results
Notes: Explain why all the tests are interesting and explain what the figures mean

## Slide 5: Experimental Realization

## Slide 6: Layer Jamming in Action
Notes: On left is no jamming

## Slide 7: Bending Test Results
Increased perforations decreases bending resistance
Increasing vacuum increases bending resistance
Creases significantly decreases bending resistance
0 perforation specimens need to be fully folded
  More broken fibers
Chart: Average Deflection from .363N Released Weight
| 0 | 0.2 | 0.4 | 0.5 | 0.6 | 0.8
-7psig | 0.072777 | 0.061741 | 0.061398 | 0.049733 | 0.061093 | 0.063411
-10psig | 0.042996 | 0.0274 | 0.025079 | 0.035008 | 0.0369 | 0.050051
-15psig | 0.022327 | 0.011405 | 0.011252 | 0.018783 | 0.023152 | 0.045199
Falling Weight Deflection for Specimen with No Crease |  |  | 
Vacuum (psig) | -7 | -10 | -15
z-Deflection (m) | 0.037 | 0.023 | 0.0086

## Slide 8: Miura Tensile Test Results
Increasing vacuum increases tensile strength
Results sensitive to folding and construction quality
Chart: Weight vs Displacement For Miura Specimen 1
| 3.4340885999999999 | 4.8741966000000003 | 5.6437812899999997 | 6.3100863000000009
-7 psig | 0.0079375 | 0.011112 | 0.011112 | 0.0127
-10 psig | 0.0047625 | 0.0079375 | 0.014287 | 0.003175
-15 psig | 0.003175 | 0.003175 | 0.0055562 | 0.014287
Chart: Weight vs Displacement For Miura Specimen 2
| 3.4340885999999999 | 5.8476429000000003 | 7.2469413000000005 | 9.6016355999999998
-7 psig | 0 | 0 | 0.0023812 | 0.0039688
-10 psig | 0 | 0 | 0 | 0.003175
-15 psig | 0 | 0 | 0 | 0
Chart: Force vs. Displacement for Miura Specimen 3
| 3.0687641999999999 | 4.5126000000000008 | 5.7009834000000001 | 7.211429100000001
-7psig | 0.375 | 0.46875 | 0.5625
-10psig | 0 | 0.3125 | 0.4375 | 0.4375
-15psig | 0 | 0.125 | 0.125 | 0.46875

## Slide 9: Closing Remarks and Discussion
The pop-through of the Hypar is preserved
  Seems to be load rate dependent
Layer jamming is an effective means for strengthening origami structures
Strict fabrication procedures must be used to ensure consistency
Any questions?